## Slide 1: 異なる親和性でのPt/n-アルカン界面の 界面熱抵抗と表面液体構造の相関
0
○ Qing-Yao Luo, Donatas Surblys, Hiroki Matsubara, Taku Ohara
日本機械学会熱工学コンファレンス2022
Oct. 8th, 2022
Institute of Fluid Science, Tohoku Univ.
Surface Liquid Structure Correlation with Interface Thermal Resistance of Pt/n-alkane Interface at Different Affinities
Notes: Good afternoon everybody. I am Qingyao Luo. Today I’m glad to be here to share my research about surface liquid structure correlation with interface thermal resistance of Pt/n-alkane interface at different affinities.

## Slide 2
Background
Thermal interface material (TIM) fills the air–gap
©mccourier
ITR is very high
ITR is decreased
Air
TIM
interface thermal resistance
size of semiconductors
density of heat dissipation
significance of ITR
Understanding thermal transport mechanism at the interface of
solid-TIM at nano scale is essential
Billions transistors in one chip
Notes: The surface of packed chip was uneven. If we connect chip and heat sink directly, there would be a air gap. Then resistance to transfer thermal energy is very high. The common method is inserting the thermal interface material. The air gap is filled then ITR is decreased. With the development of technology, billions transistors can be integrated into one chip. This causes size of semiconductors is shrunken, density of heat dissipation increased. Then ITR cannot be ignored. It is essential to understand thermal transport mechanism at the interface of solid-TIM from the micro view.

## Slide 3
merits of polymer-based TIM
Background
mechanical properties
electronic properties
chemical properties
design flexibility
low price
conformability
TIM categories
Type | Account
phase change TIMs | 4%
metallic TIMs | 9%
polymer-based TIMs | 87%
data source: BCC research
highly conductive
polymer
polymer matrix + filler
nanocomposites; nanowires
ceramic, metal,
carbon nanotube,
graphene, et.al
Notes: We can classify TIM into phase change TIMs, metallic TIMs and polymer based TIMs. The last one occupied most of market. polymer based TIM can further divided into two types: purely polymer with high intrinsic thermal conductivity. And composites of polymer matrix and filler. It owns lots of merits including good mechanical electronic chemical properties. Design flexibility. At low price. And the conformability.

## Slide 4
Existing Research on ITR of SLS System
Au-Ar-Au system
work of our group
at low affinity: ITRlarge groove > ITRsmall groove
at high affinity: ITRrough surface < ITRflat surface
at very high affinity: highly ordered liquids increase ITR
Surblys D, et al. J. Chem. Phys. 150, 114705 (2019)
work of others
Frank M, et al. J. Chem. Phys. 151, 134705 (2019)
Ag-Ar-Ag system
Same fractal dimension and depth of roughness have same ITR and liquid density profiles.
Increase roughness won’t be helpful to decrease ITR at high η.
Notes: In the previous work of our group, we researched the Au-Ar-Au systems, and find that at low affinity, ITR of large pitch is larger than small pitch; and at high affinity, ITR of rough surface is smaller than flat surface. at super high affinity, highly ordered liquids would increase ITR. Some guys researched the influence of random roughness effect on ITR

## Slide 5
Existing Research on ITR of SLS System
Au-Ar-Au system
work of our group
at low η: ITRlarge pitch>ITRsmall pitch
at high η: ITRrough surface>ITRflat surface
at η close to 1: highly ordered liquids increase ITR
Surblys D, et al. J. Chem. Phys. 150, 114705 (2019)
work of others
Frank M, et al. J. Chem. Phys. 151, 134705 (2019)
Ag-Ar-Ag system
Same fractal dimension and depth of roughness have same ITR and liquid density profiles.
Increase roughness won’t be helpful to decrease ITR at high η.
ITR of polyatomic systems should be investigated.
Objective:
Investigating surface liquid structure correlation with interface thermal resistance of Pt/n-alkane (TIM)/Pt systems at different affinities
Notes: To continue the previous work and to be closer to engineering application, we aim to investigate surface liquid structure correlation with interface thermal resistance of Pt/n-alkane (TIM)/Pt systems at different affinities

## Slide 6
Simulation System
pitch length:
0
19.575005 Å
117.45003 Å
polymer chain-length:
8, 16, 24, 36
definition of pitch
Pt-C8-Pt small pitch system
large pitch system
NEMD techniques were applied.
All The Systems:
Lx=Ly=117.45 Å
210 Å < Lz < 340 Å
Nunited-atom = 43200
Notes: Simulation system is as shown. Chain length of TIM varied from 8 to 36. We used three kinds of surfaces, flat, pitch 19.6, pitch 117.5. fig (a) is a definition of pitch, we set the depth and width of groove to be the same that the apparent area is twice of cross-section area. And we use pitch + periodic length of pitch as roughness scale. NEMD techniques were used. The leftmost layer was fixed. the second most of both sides were set as heat sink and heat source respectively. The rightmost layer was allowed to move to have polymer more freedom to interact. The number of liquid united-atom was set to be 43200 for all systems.

## Slide 7
Simulation Setting
potential models
simulation periods
Platinum solid: Morse potential (Pamuk H Ö, et al. Phys. Status Solidi A 37, 1976)
n-alkane: NERD potential (Nath S K, et al. J. Chem. Phys. 108.23, 1998)
The Lorentz-Berthelot rule is adopted to LJ interactions between sites of different types.
annealing
period
equilibration period
production
period
10ns
left wall is fixed; compress then relax the right wall gradually
8-40ns
to obtain steady heat flux;
linear temperature distribution;
small fluctuation of position rightmost wall as possible
40ns
ITR calculation:
sample every 8ns
1 fs every timestep
Notes: For solid interaction, morse model was used. polymer used nerd potential to interact. Lorentz-Berthelot rule was adopted too. about simulation procedures, anneal system firstly then equilibrate system to obtain a steady heat flux. Finally the production run was performed. We calculate ITR every 8ns, use five ITR to evaluate the error.

## Slide 8
ITR Calculation
interface position
linear fitting of T
rough surface: midpoint of rightmost layer position of not grooved section, Z1, and that of grooved section, Z2
flat surface: middle position of rightmost layer and that of first density peak
Fourier’s Law:
Notes: interface position is very import to the itr result. In this work, for rough surface systems, we choose midpoint of Z1 and Z2. Z1 is the position of rightmost layer of not grooved section. Z2 is that of grooved section. for flat systems, middle position of rightmost layer and first density peak position. Then select bulk regions to do linear fitting. And get ITR according to fourier’s law finally.

## Slide 9
Results at low affinity
ITR varies with chain-length
C8 performed best interface thermal transport ability
Roughness is not beneficial for most systems
natom ITR
ITR at different roughness scales
adsorbed atoms per cross-section area
Notes: For the itr at eta of 0.1, we found itr varies with chain-length but the apparent rule is hard to be summarized. C8 performed best interface thermal transport ability. For most systems, rough surface is not beneficial to decrease ITR.
We calculated the adsorbed atom number per cross-section area. An apparent correlation that more adsorbed atoms result into smaller ITR.

## Slide 10
Polymer Inside Grooves at low affinity
C8-pitch 19.6 & C8-pitch 117.5 & C36-pitch 117.5 can make use of additional surface area.
Most systems cannot make use of additional area due to grooving.
previous Au-Ar-Au work: all grooves were at Cassie state at low affinity
Notes: From the polymer state inside grooves, we can find most systems cannot make use of additional area due to grooving. Only C8-pitch 19.6 C8-pitch 117.5 and C36-pitch 117.5 can make use of additional surface area. This is different from our previous work for gold-argon-gold system, we found all grooves were not filled at low affinity.

## Slide 11
Results at high affinity
ITR increases with chain-length overall
ITR_pitch 117.5 < ITR_pitch 19.6 < ITR_flat
ITR_C8 close to ITR_C16
n_atom ITR
ITR at different roughness scales
adsorbed atoms per apparent area
Contradict with traditional cognition
Notes: For the results at eta of 0.5, we can saw that itr increases with chain-length overall; ITR of flat surface system is larger than pitch 19.6 system. And pitch 117.5 has minimum itr. And itr of c8 is close to itr of c16. A surprising finding is that it seems more adsorbed atoms will cause larger ITR. It is contradict with traditional cognition.

## Slide 12
Results at η of 0.5
nchain ITR
adsorbed chains per apparent area
Ohara T, et al. J. Chem. Phys. 135, 034507 (2011)
Matsubara H, et al. J. Chem. Phys. 142, 164509 (2015)
Intramolecular interaction contribution dominantes as chain-length over 16.
Transport term contribution is similar that thermal energy can be transported between solid and liquid easily because of the compact contact.
Transport term
Interaction term
intramolecular
inter-molecular
intramolecular interaction term plays an important role on the difference of interface thermal transport ability at high η
Notes: We estimated the adsorbed chains per apparent area. The trend is more adsorbed chains can decrease itr. We thinks we should care adsorbed chains rather than adsorbed atoms at high eta. Our previous work found intramolecular interaction contribution dominates as chain-length over 16. Transport term is similar because thermal energy can be transported between solid and liquid easily due to their compact contact. then intramolecular term would plays an important role on the difference of interface thermal transport ability at high eta.

## Slide 13
Polymer Inside Grooves at η of 0.5
For pitch 117.5, surfaces vertical to cross-section can adsorb chains at direction not vertical to overall heat flux direction.
ITRlarge pitch< ITRsmall pitch
adsorbed chains on surfaces
Additional area due to grooving can be made full use of .
ITRrough< ITRflat
Notes: By observing chains adsorbed on the surface vertical to cross-section, we can find lots of chains oriented at direction not vertical to the overall heat flux direction. pitch 117.5 can provide such surface while pitch 19.6 cannot. It cause itr of pitch 117.5 is smaller than pitch 19.6. from the density distribution of pitch 19 systems, we can find the additional area due to grooving can be made full use of. it explains why itr of rough systems is smaller than flat systems

## Slide 14
Conclusion
ITR is influenced by the chain-length of polymer TIM: at η of 0.1, the rule of correlation is hard to summarize; at η of 0.5, ITR increases with chain-length overall.
C8 performed best interface thermal transfer ability.
At η of 0.1: roughness is not beneficial as the additional area cannot be made full use of. In general, more adsorbed atoms result into smaller ITR.
At η of 0.5: ITR increases with chain-length overall. More adsorbed chains rather than atoms causing smaller ITR may resulted by intramolecular interaction contribution. Additional area can be made use of resulting into ITR_rough< ITR_flat. Surfaces vertical to cross-section of pitch 117.5 systems can adsorb chains at direction not vertical to overall heat flux direction resulting into ITR_pitch 117.5 < ITR_pitch 19.6.
Notes: In this work, blah blah…

## Slide 16
Existing Research on ITR of SLS System
Au-Ar-Au system
work of our group
at low η: ITRlarge pitch > ITRsmall pitch
at high η: ITRrough surface < ITRflat surface
at η close to 1: highly ordered liquids increase ITR
Surblys D, et al. J. Chem. Phys. 150, 114705 (2019)
work of others
Frank M, et al. J. Chem. Phys. 151, 134705 (2019)
Ag-Ar-Ag system
Same fractal dimension and depth of roughness have same ITR and liquid density profiles.
Increase roughness won’t be helpful to decrease ITR at high η.
To be closer to engineering application, ITR of polyatomic systems should be investigated.

## Slide 18
Liquid Structure at η of 0.1
orientation order parameter
orientation angle probability
for flat surface systems
OOP = 1: vertical to cross-section
OOP = -0.5: parallel to cross-section
No apparent correlation between OOP and ITR was found.
Notes: We estimated orientation order parameter of polymer near the interface. oop equals to 1 means chains in the slab has the orientation vertical to cross section, -0.5 means the orientation paralleling to cross-section. As oop cannot represent chain’s orientation distribution clearly, we only present flat surface systems. We also calculated the orientation angle probability density. We found the trend of each system was similar. So we think there is no apparent correlation between OOP and ITR.